Strain-tunable Ge/Si1-xGex heterostructures for hole spin qubits

Arianna Nigro1, Enrico Della Valle2, Alexander Vogel3, Eric Jutzi1, Fabian Oppliger4, Franco De Palma4, Pasquale Scarlino4, Andrea Hofmann1, Vladimir Strocov2, and Ilaria Zardo1,3

1University of Basel, Physics Department, Klingelbergstrasse 82, CH-4056 Basel, Switzerland.

2Center for Photon Science, Paul Scherrer Institut, Villigen, 5232, Switzerland.

3Swiss Nanoscience Institute, Klingelbergstrasse 82, Basel CH-4056, Switzerland.

4Hybrid Quantum Circuits Laboratory, Institute of Physics, École Polytechnique Fédérale de Lausanne (EPFL), Lausanne 1015, Switzerland.

Rapid advances in quantum information and quantum computing, driven by the demand for greater computational power, rely on the implementation of qubits as fundamental building blocks [1]. The stability, controllability, and accessibility of these qubits strongly depend on the quality of the materials hosting them, with planar Ge/Si1-xGex heterostructures emerging as one of the most promising platforms for hole-spin qubits [2]. To fully exploit the advantages of this platform, careful engineering of the heterostructure design, as well as precise control over the morphological and structural properties of its constituent layers, is essential. In particular, optimizing the strain in the Ge quantum well (QW) lifts the degeneracy between the heavy holes (HH) and light holes (LH) states in the valence band, which is beneficial for spin qubit applications [3].

In this work, we present results on the growth of epitaxial Ge/Si1−xGex heterostructures via chemical vapor deposition, using a reverse linear grading approach. Heterostructures with state-of-the-art interface sharpness between the Ge QW and the two barriers were achieved, and the degrees of freedom of the system were exploited to systematically tune the strain in the QW [4]. Strain quantification was performed using Raman spectroscopy and geometric phase analysis, and its influence on the splitting between the HH and LH bands was experimentally benchmarked via soft x-ray angle resolved photoemission spectroscopy (SX-ARPES), which was also used to determine the band offset between the Ge QW and the Si0.2Ge0.8 barrier imposed by the heterostructure design [5]. Both the transport and coupling properties of the heterostructures were assessed by successfully integrating microwave resonators and fully tunable double quantum dots on the same material stack [6].

- Burkard, G., et al. (2023). “Semiconductor spin qubits”. Reviews of Modern Physics, 95(2), 025003.

- Myronov, M., et al. (2023). “Holes outperform electrons in group IV semiconductor materials”. Small science, 3(4), 2200094.

- Scappucci, G., et al. (2021). “The germanium quantum information route”. Nature Reviews Materials, 6(10), 926-943.

- Nigro, A., et al. (2025). “Strain Engineering of Ge Quantum Wells in Planar Ge/Si1−xGex Heterostructures”. Advanced Materials Interfaces, 12(24), e00620.

- Della Valle, E., et al. (2026). “Direct observation of strain and confinement shaping the hole subbands of Ge quantum wells”. https://doi.org/10.48550/arXiv.2603.18753.

- Nigro, A., Jutzi, E., Oppliger, F., et al. (2024). “Demonstration of microwave resonators and double quantum dots on optimized reverse-graded Ge/SiGe heterostructures”. ACS Applied Electronic Materials, 6(7), 5094-5100.